## Slide 1
Pro-Electrophiles
- A source of protein-reactive extractable not covered by most screening methods -
André Stratman#, Steven A. Watt*, Lejon Martens*
#ASAS Labor GmbH, Gottfried-Hagen-Str. 60-62, 51105 Cologne
*A&M STABTEST GmbH, Kopernikusstraße 6, 50126 Bergheim
Introduction:
Screening methods to detect electrophilic extractables, which are potentially protein-reactive are well established and are readily used to screen different primary packaging components. These screening methods address protein-reactive extractables, that are either naturally electrophilic or electrophilic at the moment of extraction. However, these approaches are not predictive for extractables, which may become electrophilic as a result of oxidative aging processes.
Here we describe a novel screening approach in which, extracts of primary packaging materials are oxidatively activated to screen for components, that can be converted into potentially protein-reactive electrophiles as a result of aging processes. To simulate oxidative aging, a coulometric cell was used to convert pro-electrophilic compounds in to electrophils. As a model pro-electrophile butylated-hydroxy-toluene (BHT) was used.
Establishing the coulometric conversion of the model pro-electrophil BHT
To test the oxidative conversion of potentially pro-electrophilic extractables, BHT was treated in a coulometric cell. The activated BHT was then exposed to glutathione (GSH), a model compound used in previous studies, and reaction products were subsequently monitored by LC-MS/MS.
Fig.2: Reaction of activated BHT-QM with Angio-tensin II. Above: Extracted-ion-Chromatograms (EIC) on the MS/MS trace for the BHT-QM marker ion @ 291.18 m/z. Below: MS/MS spectra of the signals for peak group 1, 2, and 3.
Capability of oxidatively activated electrophiles to react with amines
Since there are very few free thiols available in therapeutic proteins, the results of GSH-screening assays may not be predictive for drug products in their final container closure systems.
Fig.1: Test of the reaction conditions for the oxidative conversion of pro-electrophile BHT to the electrophilic BHT-quinonemethide. Above: The reaction scheme of the oxidative conversion of BHT in a coulometric cell and the subsquent reaction of BHT-quinonemethide with GSH. Below: The LC-MS/MS analysis of the GSH-BHT Adduct.
Conclusion:
Angiotensin II + BHT
Angiotensin II + activated BHT-quinonemethide
Peak group 1
Peak group 2
Peak group 3
-BHT-QM
Δ 218.17 amu
BHT-QM marker ion @ 291.17 m/z
-BHT-QM
Δ 218.17 amu
-BHT-QM
Δ 218.17 amu
-BHT-QM
Δ 109.59 M2+
-BHT-QM
Δ 109.59 M2+
700 mV
BHT
BHT-quinonemethide
H
+
GSH
GSH-BHT-QM Adduct
GSH-BHT Adduct
Full MS
MS/MS
of 526.26 m/z
This experiment shows, that the reactions conditions in the coulometric cell are suitable to convert pro-electrophiles to electrophilic compounds capable of reacting with thiol groups in the model GSH.
Under MS/MS conditions the GSH-BHT-QM adduct loses BHT-QM, resulting in a BHT-QM marker fragment of 219.18 m/z. This marker ion may be used to identify modified peptides in full length proteins.
Therefore, the setup of oxidatively converting extractables and subsequent reaction of these with a model compound was extended to the small, thiol-free peptide Angiotensin II.
Using the BHT-QM marker ions was useful to identify BHT-QM modified peptides. Using this approach three peak groups (PG) could be identified: PG1 Angiotensin with one BHT-QM adduct at three distinct locations in the AS sequence; PG2 Angiotensin with two BHT-QM adducts; PG3 with three BHT-QM adducts.
Peak group 1
Peak group 2
Peak group 3
The oxidative activation of pro-electrohiles can be achieved in a coulometric cell. Angiotensin II can be used as a model peptide of identify electrophiles capable of reacting with amines.